PART 2 – SECTION VII

EMPLOYER’S REQUIREMENTS

Roads, Landscaping and Fences

TABLE OF CONTENTS

10	Roads, Landscaping and Fences	4

10.1	Road Works	4

10.1.1	General	4

10.1.2	Clearing and grubbing	5

10.1.3	Road formations	5

10.1.4	Sub-base construction	5

10.1.5	Road base material	6

10.1.6	Temporary reinstatement of public highways	8

10.1.7	Asphalt pavements	8

10.1.8	Bituminous course	8

10.1.9	Bituminous works	9

10.1.10	Weather limitations	9

10.1.11	Preparation	9

10.1.12	Transportation	10

10.1.13	Placing	10

10.1.14	Compaction of mixtures	11

10.1.15	Drainage	11

10.1.16	Laying kerbs and channels	12

10.1.17	Foundations for walkways	12

10.1.18	Laying concrete paving flags	12

10.1.19	Laying paving blocks	12

10.1.20	Tolerances for finished carriageway surfaces	12

10.1.21	Tiled pavements	13

10.1.22	Pre-cast units for kerbs and surface drainage	13

10.1.23	Concrete	13

10.2	Fences and Gates	13

10.2.1	General	13

10.2.2	Fences	13

10.2.3	Gates	14

10.3	Landscaping	14

10.3.1	General	14

10.3.2	Material	14

10.3.3	Existing trees	15

10.3.4	Implementation of landscaping	15

# Roads, Landscaping and Fences

## Road Works

### General

The road works in this Contract comprise construction of the following:

Service roads (The width of the service road shall be at least 5 m. If the general layout of the plant does not allow, the road width shall be subject to the Project Manager)

Parking areas

Walkways

Surface drainage for roads.

The word "roads" in these requirements includes parking areas.

Roads shall consist of the following layers:

- A layer of wearing course

- A layer of bituminous asphalt course

- A bottom layer of sub-grade material, only where necessary

- A sub-base of granular material or broken stones to a suitable grade.

Walkways shall consist of the following compacted components:

- Tiled pavements

- A bottom layer of sub-grade material, only where necessary

- A sub-base of granular material.

Walkways shall be constructed at the following locations:

- Around all buildings and structures

- Between plant roads and all plant structures

- On one side of the roads where frequent pedestrian walking is expected .

The sub-base and base in walkways shall have each a minimum thickness of 150 mm. Tiled        pavements, consisting of approved concrete slabs, shall have a minimum thickness of 50 mm. The tiles shall be laid evenly according to the lines and levels of the adjacent pavements. All tiles shall be of an approved type, design and make and shall be firmly bedded on the underlying course and shall be laid against each other. Upon completion of the tiling, sand shall be spread and shall be compacted with a mechanical vibrating machine of sufficient weight.

Sub-grade means the soil immediately below the formation. The formation and sub-grade shall be graded and compacted to the levels, falls, cambers and densities as required by DIN standards or other equivalent standards and specifications. The sub-grade shall be so compacted that the dry density of the upper 150 mm of the ground or fill is not less than 95% of the maximum dry density determined by tests in accordance with the relevant Turkish Standards. Where existing ground conditions are such that direct compaction of the sub-grade cannot be carried out as specified, unsuitable material shall be removed and replaced with granular sub-base.

The materials for the sub-base and road-base shall be laid in layers, each not exceeding 150 mm or being less than 75 mm. The total compacted thickness of the sub-base and road base shall not be less than the specified nominal thickness. The sub-base and base in roads shall have each a minimum thickness of 200 mm. Roads within the wastewater treatment plant site shall be at least 5 m wide.

### Clearing and grubbing

Clearing and grubbing for road works shall be executed according to Document No.3 of these Employer’s Requirements.

### Road formations

The road formation shall be the surface obtained after completion of any earthworks.

Formations, immediately before being covered with sub-base or road base material, shall be clean, free from mud and slurry and properly shaped and compacted to an even and uniform surface.

The preparation and surface treatment of formations shall be carried out after the reinstatement of any excavations for services.

Where unsuitable material naturally occurs at formation level, it shall be excavated as directed by the Project Manager and it shall be removed from the Site. The resulting void shall be filled with a compacted granular sub-base material, in layers not exceeding 250 mm uncompacted depth.

The sub-grade shall be compacted so that the dry density of the upper 150 mm of the ground or fill is not less than 95% of the maximum dry density. Where the sub-grade is in natural ground, the       compaction shall be carried out at or near the natural moisture content of the ground. Any               irregularities or depressions that develop in the formation during compaction of the sub-grade shall be corrected by loosening the surface of these places and adding, removing or replacing material and     re-compacting so that the surface is smooth and uniform. Any area of sub-grade that shall become muddy, broken-up or loosened due to weather conditions or otherwise damaged shall be corrected or prepared again by the Contractor as specified above.

### Sub-base construction

Within 48 hours of completion of a road formation, granular sub-base material shall be spread and compacted to the required thickness. The sub-base shall be protected from deterioration due to ingress of water, the adverse effects of weather and the use of Contractor's equipment. Compaction shall be carried out in accordance with the following table:

| Type of compaction plant | Category | Number of passes for depth layers not greater than |  |  |
| --- | --- | --- | --- | --- |
|  |  | 110 mm | 150 mm | 225 mm |
| Smooth-wheeled roller | Mass per metre width of roll: Over 2700 kg up to 5400 kg Over 5400 kg | 16 8 | Unsuitable 16 | Unsuitable Unsuitable |
| Pneumatic-tyred roller | Mass per wheel: Over 4000 kg up to 6000 kg Over 6000 kg up to 8000 kg Over 8000 kg up to 12000 kg Over 12000 kg | 12 12 10 8 | Unsuitable Unsuitable 16 12 | Unsuitable Unsuitable Unsuitable Unsuitable |
| Vibrating roller | Mass per meter width of vibrating roll: Over 700 kg up to 1300 kg Over 1300 kg up to 1800 kg Over 1800 kg up to 2300 kg Over 2300 kg up to 2900 kg Over 2900 kg up to 3600 kg Over 3600 kg up to 4300 kg Over 4300 kg up to 5000 kg Over 5000 kg | 16 6 4 3 3 2 2 2 | Unsuitable 16 6 5 5 4 4 3 | Unsuitable Unsuitable 10 9 8 7 6 5 |
| Vibrating-plate compactor | Mass per unit area of base plate: Over 1400 kg/m2 up to 1800 kg/m2 Over 1800 kg/m2 up to 2100 kg/m2 Over 2100 kg/m2 | 8 5 3 | Unsuitable 8 6 | Unsuitable Unsuitable 10 |
| Vibro-tamper | Mass: Over 50 kg up to 65 kg Over 65 kg up to 75 kg Over 75 kg | 4 3 2 | 8 6 4 | Unsuitable 10 8 |
| Power rammer | Mass: 100 kg – 500 kg over 500 kg | 5 5 | 8 8 | Unsuitable 12 |

### Road base material

Road base material shall consist of crushed rock or other material approved by the Project Manager, and shall be suitably proportioned to conform to the following grading or such other grading, where appropriate, in accordance with the requirements of the Turkish Highway Authority:

| Sieve size, mm | Percentage by weight passing square mesh |
| --- | --- |
| 75 | 100 |
| 37.5 | 85-100 |
| 20 | 60-80 |
| 10 | 40-60 |
| 5 | 20-40 |
| 2.36 | 15-30 |
| 0.425 | 5-18 |
| 0.075 | 4-9 |

The fraction passing the 0.075 mm sieve shall not be greater than two-thirds of the fraction passing the 0.425 mm sieve.

Material constituents shall comply with the following maximum limits:

For material passing the 0.425 mm sieve:

- Liquid limit:	25

- Linear shrinkage:	3

- Plasticity index:	6

For coarse material:

- Stone size:	75 mm

- Aggregate crushing value:	35%

- Water absorption:	6%

- Flakiness index:	35

- Elongation index:	35

The aggregate crushing value shall be monitored by regular testing of the material prior to its inclusion in the construction.

Road base materials shall be crushed and mixed using approved mechanical equipment to produce a material complying with the specified grading.

Water required to adjust the moisture content shall be added at the mixer. If required, the moisture content shall be adjusted to allow for evaporation loss during transportation.

Material when mixed shall be removed at once from the mixer and transported directly to the point where it is to be laid.

Road base material shall be spread evenly in a layer not exceeding 150 mm compacted thickness for the roadway and a layer not exceeding 200 mm compacted thickness in the verges. Segregation shall be avoided during transport and placing and any segregation evident after compaction shall be made good by removing and replacing with properly graded material.

Where natural gravel is used, water necessary to adjust the moisture content shall be added during  laying by use of equipment equipped with a sprinkler bar giving an even spread of water over the whole width of the pass. Uneven wetting of the road base shall be avoided by ensuring that the  equipment moves at a constant speed, and in addition, the material shall be turned over to ensure even distribution of the water throughout the layer.

The road base shall be compacted by approved equipment to a dry density which shall be not less than 95% of the maximum laboratory dry density as measured by 4.5 kg rammer method. The CBR value shall not be less than 80% after four days immersion in water.

On completion of compaction and before commencing the next operation, the surface of the granular road base shall comply with a surface tolerance of +/ -1 cm.

### Temporary reinstatement of public highways

Temporary reinstatement of public highways shall be carried out as soon as is practical after         completion of the Permanent Works and before the section of the road or pavement is re-opened for public use. Temporary reinstatement shall be maintained by making good any subsidence, shrinkage, defect, imperfection or fault a period as directed by the Project Manager but at least three months prior to final reinstatement.

Temporary reinstatement where not specifically required by the General Directorate of Highways or the Municipality shall comprise an additional depth of sub-base material as instructed by the Project Manager. Original surface materials shall be placed by hand with the wearing course upper most. The method of placing and compacting of temporary reinstatement shall be similar to that for road base construction, to the same surface tolerance, and to suit levels of the surrounding undisturbed road or pavement.

Only materials approved by the Project Manager shall be used for making good any defects.

Immediately prior to final reinstatement, the temporary reinstatement shall be cut out and disposed of offsite and the road base cut out were found to be damaged or otherwise defective and replaced and compacted as specified.

### Asphalt pavements

The final re-surfacing of asphalt public roads and pavements shall be considered as included in the rates and prices.

The Contractor shall when laying the temporary reinstatement ensure that levels of manholes and surface boxes shall match the final road surface level.

Asphalt roads within the site(s) shall be surfaced in accordance with the following herewith           Employer’s Requirements.

All the tests required by the requirements of Turkish Highway Authority shall be carried out.

### Bituminous course

The bituminous mixture for the surface courses shall conform to the requirements of locally produced mixtures.

The composition of the mixtures is generally as follows:

- Stone dust filler

- 5 to 7 % bitumen

- 70 to 75 % grey or blue calcareous material

- 23 to 25 % sand.

Bituminous mixtures shall, as far as practicable, be obtained from a local mixing plant approved by the Project Manager.

Names and addresses of local producers shall be given by the Project Manager. No bituminous mixture shall be manufactured until a job-mix formula has been submitted by the Contractor and approved by the Project Manager in writing.

The formula shall indicate the exact percentage of each sieve fraction and the exact percentage of asphalt to be used in the mixtures, including the mix temperature. The job-mix formula shall be within the master range as specified and shall be in effect until modified in writing by the Project Manager.

### Bituminous works

Bituminous Sealing

The surface of the road base shall be sprayed with suitable bitumen emulsion (M.C.70) at a rate of  1,5-2,0 kg/m² immediately after it has been completed and checked for compliance with the specified tolerances.

Bituminous Wearing Course

The laying of wearing course shall include the supply of bituminous material, the placing and       compaction of the bituminous layer and the removal of surplus material.

The wearing course shall be coated macadam, in a quality corresponding to ZTV-Asphalt with graded, broken aggregates. The layer shall be compacted by rollers.

Base Course

The laying of base course shall include the supply of bituminous material, the placing and compaction of the bituminous layer and the removal of surplus material. The base course shall comply with    ZTV-Asphalt with graded, broken aggregates. The layer shall be compacted by rollers.

Asphalt Course

The laying of the asphalt course includes the supply of material, the placing and compaction of the asphalt layer, the treatment of the completed surface and the removal of surplus material.

The asphalt course shall comply with ZTV-Asphalt with graded, broken aggregates. The layer shall be compacted by rollers to a minimum compacted thickness of not less than 4 cm. After completion fine sand shall be evenly sprayed over the surface and left for two days before final cleaning.

### Weather limitations

Bituminous courses shall be constructed only when the base is dry and when the weather is not rainy. Such courses shall not be constructed when the atmospheric temperature is below 10°C and falling, but shall be constructed when the atmospheric temperature is at least 8°C and rising, unless otherwise directed by the Project Manager.

### Preparation

Immediately before applying a bituminous pavement, the surface of the underlying course shall be thoroughly cleaned of all loose or foreign material. The underlying layer shall be coated with a tack-coat of the liquid asphalt rapid curing type (RC-250). The tack-coat to be used shall be to the Project Manager’s approval. The tack-coat shall be applied just sufficiently in advance of the placement of the asphalt concrete mixture so as to provide a thin adhesive film of bituminous cement to ensure a good bond. Tack-coat shall be asphalt emulsion (50 % water, 50% bitumen).

The tack-coat shall be uniformly applied by means of a pressure hand spray, in quantities of 0.3 liters per square meter of surface, unless otherwise directed by the Project Manager. Stakes for alignment control shall be furnished, set and maintained by the Contractor, subject to checking and correction by the Project Manager.

The stakes shall be set in lines parallel with the center line of the area to be paved, offset and spaced, as directed by the Project Manager.

Asphalt at the plant shall have minimum temperature of 150°C just before the delivery.

### Transportation

All bituminous mixtures shall be transported from the mixing plant to the spreader in trucks having tight, clean, smooth beds which have been oiled with a minimum amount of approved thin oil to    prevent adhesion of the mixtures to the trucks. Each load shall be covered with canvas, or other     suitable material, to protect it from dust or rain, and to prevent the loss of heat. Deliveries shall be arranged so that spreading and rolling of all the mixtures prepared for a day’s run can be completed during daylight, unless artificial light satisfactory to the Project Manager is provided. Any excessively wet loads shall be rejected. Hauling over freshly laid material shall not be permitted.

### Placing

The asphalt pavement shall be constructed in accordance with the thickness as present prior to removal and excavation work with a minimum thickness as specified. The temperature of each mixture when dumped into the spreader shall be as directed by the Project Manager, plus or minus 10°C. Asphalt mixture shall have a minimum of 90°C.

The spreader shall be adjusted and the speed regulated, so that the surface of the course shall be smooth and of such depth that, when compacted, it shall conform to the cross section shown on the Drawings. The length of any lane before placing the adjacent lane shall be as directed by the Project Manager. Where two spreading machines are operating in staggered position, no single lane shall be laid in advance of the adjoining lane further than shall permit a satisfactory hot longitudinal joint between the lanes.

Where forming a hot longitudinal joint, the 150 mm strip along the edge against which additional   material is to be laid shall not be rolled until such additional material is placed, except when the work is to be discontinued. After the first lane has been placed and rolled, the adjacent lane shall be placed while the unrolled 150 mm strip is hot and in readily compatible condition. Rolling of the adjacent lane shall begin along the joint. Placing of the mixture shall be as continuous as possible.

Rolling shall be carried out using at least two machines, one three wheel roller having a weight of 10 tons, and the other rubber wheel roller having a weight of 20 tones.

In areas where the use of machine spreading is impractical, the mixture shall be spread by hand and dressed with rakes. The loads shall not be dumped any faster than can be properly handled by the shovels and rakes.

Contact surfaces of previously constructed pavement kerbs, manholes and similar structures shall be painted with a thin tack-coat prior to placing the bituminous mixture.

### Compaction of mixtures

Compaction shall be affected by three-wheel rollers and tandem rollers.

Rolling of the mixture shall begin as soon as after placing as the mixture shall bear the roller without undue displacement. Delays in rolling freshly spread mixtures shall not be permitted. Initial rolling shall be affected by tandem rollers, followed immediately by the three-wheel rollers. Rolling shall start at the extreme sides of the lanes and proceed toward the center of the pavement, overlapping on     successive strips by at least one-half the width of the rear wheel of the three-wheel roller. On the          superelevated curves, rolling shall begin at the low side and progress toward the high side. Alternative trips of the roller shall be slightly different lengths. Tests for conformity with the smoothness shall be made immediately after initial compaction, any deviations in excess of the specified tolerances shall be corrected by loosening the hot surface with rakes and removing or adding material as directed    before continuing the rolling.

Generally, rolling shall be executed in such a manner as to produce a smooth surface and shall be    continued until a density of at least 100% has been obtained.

During rolling, the wheels of the rollers shall be moistened to prevent adhesion of the mixture to the wheels, but an excess of water shall not be permitted. The Contractor shall furnish additional and sufficient rollers if it is found that the pavement density specified is not obtained. In all spaces not         accessible to the roller, the mixture shall be thoroughly compacted with hot hand tampers weighing not less than 10 kg, with a tamping face of not more than 300 cm². Skin patching of an area that has been rolled shall not be permitted.

Any mixture that becomes mixed with foreign material, or is in any way defective, shall be removed, replaced with fresh mixture and re-compacted. The rollers shall not be permitted to stand on pavement which has not been fully compacted. The Contractor shall provide competent workmen who are      capable of performing all work incidentals to the correction of all pavement irregularities.

The finished surface shall not vary more than 3 mm when tested with a 3.00 m straight edge applied parallel with the center line of the pavement. After completion of the final rolling, the smoothness of the course shall be checked, and any irregularities that exceed the tolerance or that retain water on the surface, shall be corrected by removing the defective area and replacing with new pavement. The completed bituminous pavement shall be tested for thickness at such intervals as directed by the       Project Manager. Where the thickness proves to be more than 5mm smaller than the specified pavement thickness, the deficient pavement shall be removed and replaced with satisfactory pavement with no additional payment.

All joints shall present the same texture, density and smoothness as other areas of the course. The joints between old and new lanes or sections shall be carefully made in such manner as to ensure a continuous bond between the old and new pavement. All trimmed contact surfaces of previously     constructed pavement shall be painted with a thin, uniform tack coat before the fresh mixture is placed. When the edges of joints are irregular, honeycombed, or poorly compacted, all unsatisfactory sections of joint shall be trimmed to expose an even, vertical, or sharply sloping surface for the full thickness of the course. Fresh mixture shall be raked uniformly against the joint, followed by rolling; no vehicular traffic of any kind shall be permitted on the pavement for at least 24 hours.

### Drainage

Surface water drainage to site roads, hard-standings and access roads consists of a cross-fall on the surface of the roads or paved areas draining to the adjoining ground.

Where surface water drainage is provided for roads it shall consist of piped drainage. Where           practicable drainage work shall be completed before road works is commenced.

Trenches for piped drainage shall be excavated to the minimum dimensions necessary for the proper construction of the Works, and after pipes have been laid, tested and, where specified, surrounded with gravel or concrete, the trenches shall be backfilled with excavated material and compacted to a dry density equal to that of the adjacent ground. Surplus excavated material shall be disposed of offsite.

Porous pipes shall be laid dry-jointed and shall be surrounded with gravel.

Soak-away ponds and in-situ concrete catch pits with kerb weirs shall be constructed

Brickwork manholes and gullies shall be constructed complete with cast iron covers or gully gratings.

Open drainage channels for roads shall be constructed as concrete channels with a width up to 1 m and a depth up to 0.5 m. The bottom of the trench and the lower part of the slopes (1/3 of the total depth) shall receive stone pitching as described in the herewith Employer’s Requirements. The works to be carried out shall include the required excavation, the trimming, compaction and pitching of surfaces and site clearance after completion of the works.

### Laying kerbs and channels

Kerbs, edgings, channels and quadrants shall be laid and bedded on a layer of mortar, either on the concrete carriageway or on a Grade C20/25 concrete foundation. They shall be butt-jointed except where otherwise described in the Contract, save that where laid on concrete carriageways they shall be provided with joints coincident with the carriageway movement joints, of width and with filler       identical to that used in the carriageway joints. All kerbs shall be backed with Grade C20/25 concrete.

Alignment of kerbs and channels shall not deviate from that described in the Contract by more than 10 mm, with no lipping of visible faces.

### Foundations for walkways

Foundations for footways shall consist of granular sub-base material spread evenly and compacted in layers of not more than 100 mm thickness.

Compaction to the correct levels shall be carried out using a vibratory roller have a static load of at least 1000 kg/m width of roll.

### Laying concrete paving flags

Pre-cast concrete flags shall be laid to falls on sub-base material, bonded with joints at right angles to the kerb, and spot bedded with mortar with no lipping of top surfaces.

Flags shall be cut to fit around surface boxes and other furniture and, on circular work where the      radius is 12m or less, shall be radially cut on both edges to the required lines.

### Laying paving blocks

Pre-cast concrete block paving shall be used.

### Tolerances for finished carriageway surfaces

Finished surfaces at each stage of road construction shall not vary from the levels described in the Contract by more than the following permissible deviations:

| Surface | Permissible deviation, mm |
| --- | --- |
| Formation and sub-base | +10, -30 |
| Base | 15 |
| Wearing surface or slab surface | 6 |

The combination of permitted tolerances in the levels of different pavement courses shall not result in a reduction in thickness of the pavement, excluding the sub-base, by more than 15 mm from that     specified, and the maximum allowable irregularly of the wearing surface below a 3 m straight edge shall be 3 mm.

### Tiled pavements

Tiled pavements for walkways consisting of approved concrete slabs with a minimum thickness of 50 mm shall be laid on 20 mm of sand for final leveling. All slabs shall be of approved type and design and shall be firmly bedded on the underlying course and shall be laid against each other. Upon      completion of the slabs sand shall be strewed, and be compacted with a mechanical vibrating machine of sufficient weight. The application projects shall be prepared by the Contractor and shall be subject to approval of the Project Manager.

### Pre-cast units for kerbs and surface drainage

Kerbs and drains units shall be supplied and laid along the roads and parking areas to be constructed on site.

Curves shall be provided with specially made bends as follows:

Curbs shall not be laid until the 28 day strength of the pre-cast unit is attained. Kerb sections shall be set on compacted sub-grade. Any section deviating in line or level by more than 1 mm in 1 m shall be lifted and re-laid. Joints shall be grouted up with mortar. The application projects shall be prepared by the Contractor and shall be approved by the Project Manager.

### Concrete

The quality of the concrete surface course, tiled pavement, kerbs and units for surface drainage shall be according to Document No 5 of these Specifications.

## Fences and Gates

### General

The fence on concrete parapet shall surround the whole wastewater treatment plant site.

### Fences

The permanent fence shall consist of a galvanized steel wire mesh with 50 x 50 mm openings, and three rows of barbed wire above the steel mesh. Height of steel wire mesh shall be 2.40 m and the    distance between each barbed wire shall be 0.10 m. Total height of the fence 2.70 m. The poles      bearing the barbed wires bend 30 degrees from vertical to the WWTP site.

Fence poles per 3.00 m shall be galvanized iron pipe Ø 100 mm, t = 6 mm. The steel mesh shall be secured to the posts at 0.30 m intervals along the height of the posts and the chain link fence shall be supported by fixing to 3 wires strung from post to post. Furthermore, the steel mesh and posts shall be embedded in the concrete foundation.

### Gates

A sliding gate shall be installed at the entrance to the wastewater treatment plant site.

The gate shall be operated both mechanically and manually. The gate shall be operated by a control panel button in the guard house. The height of the gate shall be 1.20 m.

The gates shall be complete with all fittings such as rails, wheels, drop bolts; back catches, locking bars, lock plates and lock including three keys. The gates shall be provided with locks of the cylinder type.

## Landscaping

### General

Prior to commencement of any landscaping work, the Contractor shall submit to the Project Manager for    approval his detailed proposals for landscaping including the proposed species of grass, trees and shrubs.

### Material

Top Soil

Existing top soil stripped from the site and stored in heaps adjacent to the works shall be reused       provided it has not become contaminated and is free of rubble and debris. Where insufficient site top soil is available additional humus shall be imported from an approved source. Where the upper layer of natural soil is poor in organic matter, it shall be improved to a minimum depth of 250 mm by adding either clay or sand or silt to create a loamy soil texture consisting of 40% sand (size > 0.05 mm), 30% silt (size 0.05 - 0.002 mm) and 30% clay (size < 0.002 mm).

River Sand

River sand for use on the site shall be obtained from an approved source.

Grasses

Type of grasses shall be proposed by the Contractor and approved by the Project Manager.

Where the topsoil shall be sown with grass seed, the top 75 mm of the topsoil shall be brought to a fine tilt suitable for seeding, and sowing shall be carried out as soon as practicable after completion of top soiling having due regard to the season and the weather conditions. After the seed has been sown     uniformly, they shall be raked and lightly rolled into the surface. The young grass shall be kept free from weeds and any bare patches shall be re-seeded until an even close turf is established. The grass shall be watered and rolled as required and maintained in good condition.

Trees and Shrubs

Trees and shrubs shall be of the species proposed by the Contractor and approved by the Project Manager and shall be of the best quality and free from disease. They shall be young stock or in the case of shrubs shall be established seedlings or cuttings. All shall be sufficiently mature to survive transplanting from the supply nursery. The rood systems of all plants shall be maintained intact in the soil in which they have been grown and shall be supplied in containers.

Gravel

Gravel for use on the site for landscaping shall comply with TSE and be of 28 mm nominal size.

### Existing trees

Inspection of Retained Trees

All trees and shrubs to be retained shall be inspected jointly by the Project Manager and the Contractor at the commencement of the Contract and a list of trees to be retained shall be agreed. Any tree found to be diseased, dead, dying or unsafe shall be felled and uprooted subject to the prior approval of the        Project Manager.

Tree Felling

Existing trees and shrubs were directed by the Project Manager shall be cut down and all stumps and main roots shall be grubbed up. All planting thus dealt with shall be either burnt in situ or removed from the Site. The removed trees place should be transported to the place by the Employer.

Protection of Retained Trees

During execution of works existing trees and shrubs that are to be retained shall be adequately protected from all operations and from animals. Small trees and shrubs generally shall be surrounded by    adequate temporary fencing to safeguard trunks and foliage. Large trees shall have suitable screening round trunks, and low branches shall be protected by temporary fencing or barriers to prevent damage. Construction materials shall not be stored close to or within the branch spread of any tree or shrub. Existing ground levels shall be maintained.

Maintenance of Retained Trees

Retained trees and shrubs shall be maintained during the Contract and pruned at completion having due regard to the appropriate time of year for such work to be carried out. Maintenance shall include removing snags, dead wood and fronds, sealing cavities and irrigating as required to ensure the       continued health of existing planting.

Replacement of Damaged Trees

Should any retained tree or shrub be damaged as a result of the building operations then it shall be    replaced by the Contractor by an equivalent mature tree or shrub of the same variety.

### Implementation of landscaping

Preparation of Ground

The areas to be landscaped shall be brought to final ground levels less the depth required for top soil or other surfacing and all surplus material shall be disposed of offsite.

Cultivation of Ground

The Contractor shall relay 250 mm thick topsoil. Any deficiency in the topsoil shall be made up with imported top soil. Prior to replacing topsoil areas of the Site which are to be prepared for grass     planting shall be thoroughly broken up by deep raking and cross raking to a depth of 450 mm.         Retained topsoil shall be used as filled to final ground level subject to the approval of the Project Manager being first obtained. Imported top soil shall be used if the existing top soil is insufficient or unsuitable. Where new and replacement trees or shrubs are to be planted in agreement with the Project Manager, holes 1 m deep below final ground level shall be excavated in each case. These shall be filled with sweet and topped with 250 mm of top soil. Sand filling shall be thoroughly mixed with 10 kg manure before placing.

Time for Planting

In programming the planting work the Contractor shall take due regard of the accepted seasons for planting.

Top Soil Dressing

Top soil ready to receive planting shall be given a dressing of manure at a rate of 5 kg/m².

Supply of Plants

All trees, shrubs, grasses and other plants shall be supplied by the Contractor based on the Landscape design to be prepared by the Contractor and approved by Project Manager.

Planting of Trees and Shrubs

Prior to planting holes for trees and shrubs shall be prepared and filled twice with water. Plants shall be watered in their containers so that the soil and the roots are kept in a moist condition. Plants shall then be removed from their containers and their root ball complete with soil set in place and the holes backfilled and the plants firmly trodden in. Soil shall not be allowed to rise above the original        container level and the ground level around the trunk or stem shall be set below adjacent ground to retain irrigation water. All species of tree and shrubs where required shall be provided with supports during planting. These shall take the form of timber stakes of adequate strength driven into the ground adjacent to the trunk or stem without damage to roots. Wide hessian strips shall be used to tie the plant securely but no tightly to the support. Where shrubs are to be planted in groups to provide ground   cover, individual plants shall be spaced as follows:

| Size | Height when grown | Spacing |
| --- | --- | --- |
| Small | Less than 1 m | 500 - 600 mm |
| Medium | 1 - 2 m | 900 - 1200 mm |
| Large | Over 2 m | 1800 mm |

Irrigation

After planting of native tree and shrub species they shall only be irrigated twice and thereafter only as required. Non-indigenous species shall be irrigated regularly until handover to the Employer. Grassed areas shall be irrigated immediately after planting and regularly thereafter until handover. Watering of grass shall be by night time sprinkler system.

Maintenance

All new plants and grassing shall be maintained after planting. This shall take the form of irrigation, restacking, pruning, weeding, tilling, etc. to ensure sufficient growth is achieved by all. Once grassed areas are sufficiently established, they shall be kept cut or mown to provide a uniform depth of growth. Edges of grassed areas shall be trimmed as necessary. All new plants and grassed areas shall be      protected to prevent damage from workmen, builders’ plant, equipment and animals, by the use of temporary fencing or other suitable means.

Replacement

Any trees, shrubs or areas of grass which fail to satisfactory growth or wither and die shall be         replaced. The responsibility for the irrigation and maintenance of these replacement plants shall remain with the Contractor until such time as they exhibit satisfactory growth.